Technical Parameter Report

| Count :20s/2 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:59.05 Strength:2300CN Elongation%: 15.55 TPM:580 | Count :20s/3 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:88.58 Strength:3400CN Elongation%: 13.909 TPM:460 |
| --- | --- |
| Count :30s/2 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:39.37 Strength:1500CN Elongation%: 14.22 TPM:650 | Count :30s/3 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:59.05 Strength:2200CN Elongation%: 14.772 TPM:570 |
| Count :40s/2 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:29.53 Strength:1100CN Elongation%: 14.04 TPM:800 | Count :40s/3 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:44.29 Strength:1700CN Elongation%: 14.464 TPM:650 |
| Count :50s/2 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:23.62 Strength:860CN Elongation%: 13.1 TPM:850 | Count :50s/3 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:35.43 Strength:1350CN Elongation%: 11.732 TPM:750 |
| Count :60s/2 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:19.68 Strength:700CN Elongation%: 13.47 TPM:900 | Count :60s/3 Raw Material: Yizheng bright(1.33dtex×38mm) Weight:29.52 Strength:1150CN Elongation%: 11.584 TPM:820 |

Hubei Mingren Dongfang Industry & Trade Co., Ltd.

Room1402,Block 5 ,Fanhai International CBD,No.62 Zhujiang Road ,Wuhan,Hubei,